Biomaterial a Boon to Hernial Repair in the field of Veterinary Surgery

Abdul Mohsina1, Paramasivam Tamilmahan1*, Dayamon D. Mathew1, Vellachi Remya1, Ninu Ajantha Ravindran1, Naveen Kumar1, Swapan Kumar Maiti1, Kumaragurubaran Karthik2, Manjunathachar Haranahalli Vasanthachar3

1Division of Veterinary Surgery, 2Division of Veterinary Bacteriology and Mycology, 3Division of Veterinary Parasitology

*Corresponding author: drtamilmahan.bison@gmail.com

Indian Veterinary Research Institute, Izatnagar, India-243122

Abstract

Hernia is found to be one of the common surgical affections in veterinary patients and its treatment has gone through a series of gradual changes from simple herniorrhaphy to hernioplasty in case of voluminous hernias and large abdominal wall defects. Because of the complications encountered in the use of synthetic materials in hernioplasty they are now being replaced by biological materials like acellular dermal grafts, acellular diaphragm, acellular aorta etc., and they are found to be effective and better than synthetic ones in many respects. Skin fibroblasts possess the capacity to inhibit the invitro proliferation of T lymphocytes. Fibroblasts also secrete modulatory molecules like PGE2 and nitric oxide, similar to mesenchymal stem cells (MSC). Stem cell seeded bioengineered acellular grafts proved to be more effective as they reduce the immunogenicity of grafts and this seems to be a growing field in hernial treatment. This review article discusses prosthesis and use of acellular collagen matrices in hernia repair, tissue engineering, decellularization and use of fibroblast seeded scaffolds in hernioplasty.

Keywords: Hernia, Biomaterial, Tissue Engineering, Decellularization

Introduction

Hernia is defined as the protrusion of the contents of a body cavity through a normal or abnormal opening in the wall of that cavity either to lie beneath the intact skin or to occupy another adjacent body cavity. The herniated structure is covered by the parietal peritoneum, called the hernial sac, while protruding through the hernial ring (Malangoni and Rosen, 2007). Abdominal hernia is a term used to describe a hernia through any part of the abdominal wall other than a natural orifice. Small hernial ring with reducible hernial contents can be treated by conventional methods (Stock, 1954). Repair of large abdominal wall defects and voluminous hernias in animals encounter great difficulties mainly due to large size of the hernial ring and exaggerated distension of hernial margin. Recurrence in these cases occurs frequently and the deformity gets even worse because of inadequate tissue at the site to enable a satisfactory closure. These problems can be overcome by use of special methods like hernioplasty with implantation of biomaterials.

The surgical procedure for reconstruction of abdominal wall defects has gone through a series of changes.  Previously abdominal wall defects were reconstructed by simply apposing muscles later came the era of synthetic prosthetics and meshes. The most frequent complication leading to implant failure and recurrence is infection of the surgical site (Ingle-Fehr et al., 1997). To avoid these complications, the prosthetic material should be inert, but it should also support fibroplasia (Johnson, 1969). Mesh repair proved to be superior to suture repair resulting in lower recurrence and less abdominal pain and complications (Burger et al., 2004; Penttinen and Gronroos, 2008).

Meshes can be placed either intraperitoneally or extraperitoneally.In the latter it can be placed either as inlay or outlay. The prosthetic material can be fixed simply by physical pressure between the abdominal wall layers (Stoppa and Rives, 1984), by suturing with non-absorbable material (Lichtenstein et al, 1989), absorbable material (Gianlupi and Trindade, 2004), clips (Read, 2011) or fibrin glue (Agresta and Bedin, 2008; Negro et al., 2011). Advantages of inlay technique are minimal soft tissue dissection, thereby reducing devascularised tissue and its disadvantage is high rate of recurrence. Outlay technique is having disadvantage of vast soft tissue dissection (Penttinen and Gronroos, 2008). First biomaterial for hernia repair was silver mesh described by Witzel (1900). Later other materials were introduced like nylon (Acquaviva and Bourret, 1944), perlon (Kneise, 1953), polyethylene (Usher, 1958), silk mesh (Handley, 1963), etc. Among synthetic materials polypropylene is a suitable material for abdominal wall defect repair, because of the inert nature it can be used even in presence of infection and contamination (Vilar et al., 2009).

Collagen is regarded as one of the most useful biomaterial due to its excellent biocompatibility, biodegradability and weak antigenicity (Lee et al., 2001). Immunological reaction of the cellular graft may be due to the presence of histocompatibility antigens in the cells (Gulati and Cole, 1994). Cartmell and Dunn (2000) advocated the reduced antigenicity of acellular grafts. Gulati and Cole (1994) observed less immunogenicity and better tolerance of acellular grafts in rats and rabbits. Zhang et al., (2002) also found xenogenic acellular dermal matrix an ideal material with good compatibility feature and low absorptivity.

Fibroblasts play an important role in regeneration of new tissues due to their growth accelerating property of tissue cells by secreting several growth factors and extra cellular matrix (ECM).  Primary mouse embryonic fibroblasts (p-MEFs) have a number of properties making them an attractive cell culture model. Comparing to other primary explant cultures they are easy to establish and maintain, proliferate rapidly resulting in large numbers of cells produced from a single embryo within several days (Garfield, 2010). Major Histocompatibility Complex (MHC) Class II antigens are present on the transplanting cells which is responsible for graft rejection. Fibroblasts lack these surface molecules and this makes them relatively immunologically inert. Seeding of fibroblasts on the biomaterials not only improved healing time but also the cosmetic appearance (Lamme et al., 2000).

Prosthesis in hernia repair

Prosthesis for the repair of large abdominal wall defects can be done by both synthetic and biological materials. The different synthetic materials used are polyester fabric (Shoukry et al., 1997), nylon, Dacron and stainless steel (Kanade et al., 1988; George and Mohammad, 1993), cotton mesh (Kanade and Kumar,1990), mosquito net mesh (Stephenson and Kingsnorth, 2011), vicryl mesh (Buchsbaum et al., 1985), polypropylene mesh (Kassam et al., 2014), expanded polytetrafluro ethylene (PTFE) (Kennedy and Matyas, 1999; Gillion et al., 1999), mersilene mesh (Riply and Mc Carnon,1994), Carbon fibers and Carbon sheet (Gangwar, 2002), oxidized generated cellulose, polyethylene glycol and hylan G-F20 (Altinli et al., 2011). A synthetic non-absorbable material Polypropylene mesh (PP), is the most widely used material for abdominal wall replacement and reinforcement during hernia repair (Bastos et al., 2006).

Prosthetic materials can be absorbable or non-absorbable. Non-absorbable synthetic meshes like polypropylene and PTFE provide good mechanical strength, but synthetic non-absorbable materials in abdominal wall defect repair can lead to complications like bowel adherence and obstruction, fistula development, wound infection and seroma/ hematoma formation (Aldridge and Simson, 2001; Losanoff et al., 2002; Korenkov et al., 2002; Besim et al., 2002). Because of the complications encountered in the use of synthetic materials in hernioplasty they are now being replaced by biological materials like acellular dermal grafts (Gangwar, 2002; Purohit, 2008), acellular diaphragm (Perme, 2007; Kaarthick, 2011), acellular aorta (Kumar et al., 2012) etc., and they are found to be effective and superior than synthetic ones in many respects.

As an alternative biological materials can be used in the repair of defect. But cellular grafts may cause immunological reactions due to the presence of histocompatible antigens. These complications can be prevented by use of decellularized matrices and these are the latest alternative in this series. Biological materials reported to be used are small intestine mucosa and acellular dermis (Dalla-Vecchia et al.,1999; Avella et al., 2011), tensor fascia lata, rectus abdominis fascia, latissimus dorsi muscle (Brennman et al.,1995), human duramater (Takahashi et al.,1994), porcine dermal collagen (Zhang et al., 2003), diaphragm ( Varshney et al., 1990), autologus full thickness skin and dermis (Bhattacharya and Bose, 1998), decellularized porcine small intestinal submucosa (Turner et al., 2011), human acellular dermis (Bellows et al., 2007), human acellular collagen matrix (Dufrane et al., 2008), acellular dermal graft and glutaraldehyde treated acellular dermal graft (Gangwar, 2002), porcine acellular dermal matrix and porcine small intestinal submucosa (Liu and Bhatia, 2002; Zhang et al., 2003), collagen scaffolds loaded with collagen binding basic fibroblast growth factor (Shi et al., 2011), fibroblast seeded PLLA (poly lactic acid) 3D scaffolds (Pu et al., 2010) decellularized dermal scaffolds seeded with autologus bone marrow derived mesenchymal stem cells (Zhao et al., 2012). Bovine parietal peritoneum for repair of ventral hernia in rat model was successfully done by Bastos et al., (2006).

Advantages of biological materials include their capacity to resist infection and induce a milder inflammatory response, angiogenesis and host cell migration. Their disadvantages are their high cost, rapid break down, loss of graft material especially in the infected fields and undesirable host foreign body reaction (Bellows et al., 2007). Acellular collagen rich tissue matrices are prepared by physical, chemical or enzymatic manipulation of different tissues like bone, skin, blood vessel wall, bladder submucosa, small intestinal submucosa etc. (Yoo et al., 1998; Chen et al., 1999).  These matrices were observed to have less immunogenicity and better tolerance due to their reduced antigenicity (Gulati and Cole, 1994). Antigenic epitopes, damage associated molecular pattern (DAMP) and DNA molecules present in the biological matrices are removed by decellularization and chemical cross-linking process (Bianchi, 2007; Lotze, 2007). p-MEF or mesenchymal stem cells seeded biological scaffolds are widely used now a days. p-MEFs act as a feeder layer as it secretes the necessary factors required for development of other cell types and it is having high proliferative and regenerative capacity (Garfield, 2010). In the surgical treatment of skeletal muscle restoration, biological scaffolds represent a promising option

Tissue Engineering

A commonly used definition of tissue engineering as stated by Langer and Vacanti (1993) is "an interdisciplinary field that applies the principles of engineering and life sciences toward the development of biological substitutes that restore, maintain, or improve tissue function or a whole organ". Tissue engineering has also been defined as "understanding the principles of tissue growth, and applying this to produce functional replacement tissue for clinical use." (MacArthur and Oreffo, 2005)

Tissue engineering is the use of combination of cells, engineering and materials methods, and suitable biochemical and physio-chemical factors to improve or replace biological functions. While it was once categorized as a sub-field of biomaterials, having grown in scope and importance it can be considered as a field in its own right. While most definitions of tissue engineering cover a broad range of applications, in practice the term is closely associated with applications that repair or replace portions of or whole tissues (i.e., bone, cartilage, blood vessels, bladder, skin, muscle etc.). Often, the tissues involved require certain mechanical and structural properties for proper functioning.

The two major approaches in developing engineered tissue are the in-vitro and in-vivo methods. The in-vitro attempts to create organs in tissue culture or bioreactors for implantation and replacement of diseased or damaged tissue, and has received the most attention from the lay press. The in-vivo approach attempts to create an acellular biomaterial that contains clues conductive for tissue cell recruitment into the biomaterial and inductive of cell differentiation to form the needed tissue. Regardless of whether the biomaterial contain cells or not, many fabrication engineered for implantation contain bioactive and a biopolymer backbone. Bioactives are selected to stimulate tissue cells to migrate and proliferate and ultimately to differentiate. The biopolymers typically provide mechanical support for cell migration and proliferation. However then prepared from natural ECM, these scaffolds and hydrogels may provide additional biological stimuli to support cell and tissue function (Lutolf and Hubbell, 2005). Different functions provided by engineered tissue are structural (bone, cartilage, and skin) or metabolic      (liver, pancreas), or both (Chapekar, 2000).

The engineered bioactive-biopolymer construct and tissue cells, whether preloaded or host-derived, reciprocity for further tissue development (Nelson and Bissell, 2006). However collagen-based biomaterials are of the utmost importance for tissue engineering and regenerative medicine.  Because  of  its  superior  biocompatibility  and  low  immunogenicity,  collagen  is  still  the  protein  of  choice  for  biomaterials  preparation.  It  can  be  extracted  from  various  tissue  sources  and  assembled  in  combination  with  other  molecules.  There  is  also  a  use  in  the  laboratory  as  a  decellularized ECM in fundamental studies or as tissue replacement material in medical applications. Tissue engineering has progressed rapidly in recent years and has now emerged as a potential alternative to tissue or organ transplantation (Chapekar, 2000). It has provided drastic advances in all fields of surgery like ophthalmology (Chirila,2010; Hashimoto et al., 2010; Pang et al., 2010; Trese et al., 2012), orthopedic surgery (Ivkovic et al., 2011; Mahapatra and Khan, 2011; Khan et al., 2012), dental surgery (Bohi et al., 1998; Balasundaram et al., 2012; Payne, 2014), soft tissue surgery (Black et al.,1998), cardiovascular surgery (Schoen, 2011; Kurobe et al., 2012; Lam and Wu, 2012; Moroni and Mirabella, 2014) and neurosurgery (Huang et al., 2009; Cullen et al., 2011; Aronson et al., 2012;).

Biomaterials

A biomaterial is any material, natural or man-made, that comprises whole or part of a living structure or biomedical device which performs, augments or replaces a natural function. The development of biomaterials, as a science, is about fifty years old. The study of biomaterials is called biomaterial science. Biomaterial science encompasses element of medicine, biology, chemistry, tissue engineering and material science. The ideal characteristics of a biomaterial are it should be inert completely, it should have sufficient strength to hold during healing, should have good handling characteristics, should be easily sterilisable, should be non-toxic, non-carcinogenic, non-teratogenic and inexpensive (Rousch, 2003).

Extracellular matrix constitutes a complex mixture of structural and functional proteins that remains after removal of cells from a tissue or organ (Gilbert et al., 2006). Biological scaffold materials are composed of extracellular matrix. Extracellular matrix (ECM) consists of the structural and functional molecules secreted by the resident cells of each tissue and organ from which they are prepared (Badylak et al., 2009). The glycosaminoglycans (GAGs) are important components of ECM and play important role in binding of growth factors and cytokines, water retention and the gel properties of the ECM (Badylak, 2002).

Collagen based implants have been widely used as vehicles for transportation of cultured skin cells or drug carriers for skin replacement and burn wounds (Boyce, 1998; Kaarthick, 2011; Singh et al., 2011)

ECM exists in all tissues and organs but can be harvested for use as a therapeutic scaffold from relatively few sources. The extracellular matrices have been derived from variety of tissues like small intestinal submucosa ( Kumar, 2010; Aachoui and Ghosh, 2011), urinary bladder (Zhu et al., 2010; Dewangan, 2010; Eberli., 2011; Haichao, 2013), tendons (Longo et al., 2010; ), ligaments (Kew et al., 2011), tracheal matrix (Zhang et al., 2012), pericardium, diaphragm (Perme, 2007; Kaarthick, 2011), skin (Purohit, 2008), fish swim bladder (Kumar, 2010; Remya, 2012)  for tissue engineering.

The functional requirements of dermal substitutes are, it should protect the wound from infection and loss of fluid, provide a stable and biodegradable template for the synthesis of neodermal tissue, either host or enable the influx of cells that will function as dermal cells, producing dermal tissue rather than scar tissue and allow ease of handling and resist tear forces (Van der Veen et al., 2010). The biological scaffold materials are biodegradable unless processed in such a manner that irreversible cross-links are created between the resident molecules (Badylak et al., 2009).

DeSagun et al. (2001) judged the efficacy of xenogenic and allogenic acellular dermal matrix in the repair of full thickness skin defects on dorsum of rats on the basis of gross and immunological observations. In the defect implanted with xenogenic acellular dermal matrix, a short lived acute inflammatory response, long lasted humoral and cell mediated immune response and poor wound healing were observed. The healing was significantly better in allogenic acellular dermal matrix. Rennekampff et al. (1997) observed that acellular dermal matrix could effectively direct the regeneration of normal skin morphology. Erkin et al. (2007) observed the revascularization potential of xenogenic acellular dermal matrix (alloderm) in rats and Tohyama et al., (2009) found the same in tendon grafts.

The porous collagen scaffold for treating dermal wound application was developed and the wound healing was observed in a shorter time (Falanga et al., 2007).

Decellularization

A decellularization protocol generally begins with lysis of the cell membrane using physical treatments or ionic solutions, followed by separation of cellular components from the ECM using enzymatic treatments, solubilisation of cytoplasmic and nuclear cellular components using detergents, and finally removal of cellular debris from the tissue. These steps can be coupled with mechanical agitation to increase their effectiveness (Gilbert et al., 2006). The alkaline and acid treatments are used in decellularization protocols to solubilize the cytoplasmic component of the cells as well as remove nucleic acids such as RNA and DNA. Porcine small intestinal submucosa has been decellularized using peracetic acid (PAA) at concentrations of approximately 0.10–0.15% (w/v). This treatment was highly efficient at removing cellular material from these thin ECM structures, and simultaneously disinfected the material by entering microorganisms and oxidizing microbial enzymes (Hodde and Hiles, 2002).

Conventionally, two strategies have been used to alleviate rejection of these substances. One of the two strategies was to reduce the immune reaction of hosts and the other was to reduce the antigenicity of allografts or xenografts mainly by cross-linking (Rosenberg et al., 1987). Yannas (1996) demonstrated that the immunogenicity of the collagen was measurable but the actual significance of such immunogenicity was very low due to small species difference among different types of collagen. Both residual cellular debris and extracellular matrix protein in glutaraldehyde treated tissue were thought to contribute such an immune response (Coito and Kupiec-Weglinsky, 1996). The acellular grafts were less immunogenic having better tolerance by allogenic hosts and equally effective as isograft (Gulati and Cole, 1994; Nagao et al., 2011).

Decellularized tissues and organs have been successfully used in a variety of tissue engineering/ regenerative medicine applications and the decellularisation methods used vary as widely as the tissues and organs of interest, the efficiency of cell removal from a tissue is dependent on the origin of the tissue and the specific physical, chemical and enzymatic  methods that are used. Each of these treatments affects the biochemical composition, tissue ultrastructure and mechanical behavior of the remaining ECM scaffold, which in turn, affect the host response to the material. The goal of a decellularisation protocol is to efficiently remove all cellular and nuclear material while minimizing any adverse effect of the composition, biological activity and mechanical integrity of the remaining ECM (Gilbert et al., 2006).

Decellularization can be brought about by chemical, enzymatic and mechanical method which leaves a material composed of extracellular matrix components. These acellular tissues retained their natural mechanical properties and promoted remodeling of the prosthesis by neovascularization and recellularization by the host (Schmidt and Baier, 2000). The cells in extracellular matrices have class I and II histocompatibility antigens capable of eliciting rejection reactions. Also, the cells have glycoproteins recognized by the immune system of hosts, which elicit rejection reactions. Therefore, if these substances are eliminated from extracellular matrices, rejection reactions can be prevented. However, complete elimination of all antigens is considerably difficult to perform and verify (Malone et al., 1984; Wong and Griffiths, 2014).

Physical method of decellularisation includes snap freezing (Wang et al., 2012; Sheridan et al., 2013), mechanical agitation and sonication, applying direct pressure (Freytas et al., 2004). The chemical method of decellularisation includes use of acid and alkaline agents, Non-ionic detergents like triton X-100, ionic detergents like sodium dodecyl sulfate, triton X-200, zwitter ionic detergents like 3-[(3-cholamidopropyl)dimethylammonio]-1-propanesulfonate (CHAPS), sulfobetaine-10 and -16 (SB10, SB-16), Tri(n-butyl) phosphate, hypotonic and hypertonic solutions. The enzymatic method of decellularisation includes use of trypsin, endonucleases and exonucleases (Gilbert et al., 2006).

Ionic detergents are effective for solubilizing both cytoplasmic and nuclear cellular membranes, but tend to denature proteins by disrupting protein–protein interactions (Seddon et al., 2004). Sodium deoxycholate is very effective for removing cellular remnants, but tends to cause greater disruption to the native tissue architecture when compared to sodium dodecyl sulphate (Gilbert et al., 2006). The osmotic shock with a hypotonic solution such as deionized water is used to lyse the cells within tissues and organs (Woods and Gratzer, 2005).

Fibroblasts

The fibroblasts are common cells present in the connective tissue that synthesizes and continuously secretes precursors of extracellular matrix like collagens, glycosaminoglycans, reticular and elastic fibers and glycoproteins in mammalian tissues. Skin fibroblasts possess the capacity to inhibit the invitro proliferation of T lymphocytes. Fibroblasts also secrete modulatory molecules like PGE2 and nitric oxide, similar to MSC (Bouffi et al., 2011).

Fibroblasts can be induced to produce a thin three dimensional sheet of ECM material in-vitro (Ishikawa et al., 1997; Sakai et al., 2013). Fibroblasts remodel the collagen matrix from dendritic to stellate/bipolar, and cell matrix interactions mature from punctuate to focal adhesion organization. Divya and Nandakumar (2006) found that collagen is chemotactic for fibroblasts and it enhances fibroblast attachment through its scaffold like fibrillar structure and stimulate platelet degranulation, thereby accelerating fibers and clot attachment. Fibroblasts grown on DMEM media were found to be spindle shaped, elongated and bipolar in nature and were having extensive projections showing contacts with neighbouring cells. Dubay et al., (2004) reported reduced development of primary incisional hernias from 60 to 30% and recurrent incisional hernias from 80 to 23% by the implantation of a fibroblast growth factor releasing polyglactone polymer rod into the fascial wound of rat. Type 1 collagen staining was also significantly increased in bFGF treated fascia. Patient’s hernia sac, when used as a biomaterial to correct hernia reinforced surgery since it induced fibroplasia (Silva et al., 2004). Stem cell seeded bioengineered acellular grafts proved to be more effective as they reduce the immunogenicity of grafts and this seems to be a growing field in hernial treatment.

Conclusion

Collagen based biomaterials are found to be excellent graft material for hernioplasty. They can be prepared from a variety of biological materials like skin, diaphragm, aorta, tensor fascia lata, latissimus dorsi muscle etc. Acellular collagen rich tissue matrices are prepared by physical, chemical or enzymatic manipulation of these tissues. Advantages of biological materials include their capacity to resist infection and induce a milder inflammatory response, angiogenesis and host cell migration. Stem cell seeded bioengineered acellular grafts proved to be more effective as they reduce the immunogenicity of grafts and this seems to be a growing field in hernial treatment. Biomaterials have been a gift to the field of surgery involving hernias as they can provide the support and strength in case of larger hernia defect.

ACKNOWLEDGEMENTS

Authors are highly thankful to the Director of the Institute for providing necessary facilities

ReferencesCollagen Dressing Versus Conventional Dressings in Burn and Chronic Wounds: A Retrospective StudyTissue Engineering in Orthopaedics and Musculoskeletal Sciences

- Acquaviva DE and Bourret P (1944). Cure d’une volumineuse éventration par plaque de nylon. Bull. Med. Soc. Chir. Marseille. 5: 17.

- Agresta F and Bedin N (2008). Transabdominal laparoscopic inguinal hernia repair: is there a place for biological mesh? Hernia. 12: 609–612.

- Aldridge AJ and Simson JN (2001). Erosion and perforation of colon by synthetic mesh in a recurrent paracolostomy hernia. Hernia. 5: 110-112.

- Altinli E, Sumer A, Koksal N, Onur E, Senger S, Eroglu E, Celik A and Gumrukcu G (2011). Prevention of adhesion to prosthetic mesh: comparison of oxidized generated cellulose, polyethylene glycol and hylan G-F20. Ulus. Travma. Acil. Cerrahi. Derg. 17: 377-382.

- Anant Mahapatra and Wasim S Khan (2011). Tissue engineering in orthopaedics and musculoskeletal sciences. Open Orthop J. 5:239–241.

- Badylak SF (2002). The extracellular matrix as a scaffold for tissue reconstruction. Cell Dev. Biol. 13: 377-383.

- Badylak SF, Freytas DO and Gilbert TW (2009). Extracellular matrix as a biological scaffold material:structure and function. Acta Biomater. 5: 1-13.

- Bastos ELS, Fagundes DJ, Taha MO, Novo NF, Juliano Y, Simoes MJ and Silvado RAB (2006). The role of bovine preserved peritoneum in rats ventral hernia. A histological evaluation. Acta. Cir. Bras. 21: 328–331.

- Bellows CF, Albo D, Berger DH and Awad SS (2007). Abdominal wall repair using human acellular dermis. Am. J. Surg. 194:192–198.

- Besim H, Yalcin Y, Hamamci O, Arslan K, Sonisik M, Korkmaz A and Erdogan S (2002).  Prevention of intra-abdominal adhesions produced by polypropylene mesh. European Surg. Res. 34: 239-43.

- Bhattacharya S and Bose PK (1998). Autologus full thickness skin and dermis as suture and graft in dog. Indian Vet. J. 75: 1028-29.

- Bianchi ME (2007). DAMPs, PAMPs and alarmins: all we need to know about danger.   J. Leukoc. Biol. 81:1–5.

- Black AF, Berthod F, L’Heureux N, Germain L and Auger FA (1998). In-vitro reconstruction of a human capillary-like network in a tissue engineered skin equivalent. FASEB J. 12: 1331–40.

- Bohi KS, Shon J, Rutherford B and Mooney DJ (1998). Role of synthetic extra cellular matrix in development of engineered dental pulp. J. Biomater. Sci. Polymer  9: 749–64.

- Bouffi C, Bony C, Jorgenson C, Noel D (2011). Skin fibroblasts are potent suppressors of inflammation in experimental arthritis. Ann. Rheum. Dis. 70(9): 1671.6

- Boyce ST (1998). Skin substitutes from cultured cells and collagen-GAG polymers. Med. Biol. Eng. Comput. 36: 791-800.

- Brennman FD, Boulanger BR and Antonyshyn O (1995). Surgical management of abdominal wall disruption after blunt trauma. J. Trauma. 39: 539-544.

# Brian M Stephenson, Andrew N Kingsnorth (2011). Safety and sterilization of mosquito net mesh for humanitarian inguinal hernioplasty. World J. Surg. 35:1957–1960.

- Buchsbaum HJ, Chiristopherson W, Lifshitz S and Bernstein S (1985). Vicryl mesh in pelvic floor reconstruction. Arch. Surg. 120: 1389-91.

- Burger JW, Luijendik RW, Hop WC, Halm JA, Verdaardonk EG and Jeekel J (2004). Long term follow-up of a randomized controlled trial of suture versus mesh repair of incisional hernia. Ann. Surg. 4: 578-85.

- Chapekar MS (2000). Tissue Engineering: Challenges and Opportunities. J. Biomed. Mater. Res. Appl. Biomater. 53: 617–20.

- Chirila TV (2010). An introduction to ophthalmic biomaterials and their application through tissue engineering and regenerative medicine. In Traian Chirila (Ed.),Biomaterials and regenerative medicine in ophthalmology (pp. 1-13) Boca Raton, Oxford: CRC Press, Woodhead.

- Coito AJ and Kupiec-Weglinsky JW (1996). Extracellular matrix protein bystanders or active participants in the allograft rejection cascade? Ann. Transplant. 1: 14-18.

- Cullen DK, Wolf JA, Smith DH, Pfister BJ (2011). Neural tissue engineering for neuroregeneration and biohybridized interface microsystems in vivo (part 2).  Crit. Rev. Biomed. Eng, 39(3): 241-259.

- Dalla-Vechhia L, Engum S, Kogon B, Jensen E, Davis M and Grosfeld J (1999). Evaluation of small intestinal sub mucosa and acellular dermis as diaphragmatic prosthesis. J. Pediatr. Surg. 34: 167-71.

- DeSagun EZ, Botts JL, Srivastava A, Hanumadass M and Walter RJ (2001). Long term outcome of xenogenic acellular matrix implantation in immunocompetent rats. J. Surg.  Res. 96: 96-101.

- Dewangan R (2010). In-vitro and in-vivo biocompatibility testing of xenogenic bladder acellular matrix graft n a rabbit model. Ph.D. thesis submitted to Indian Veterinary Research Institute, Deemed University, Izatnagar, Bareilly, Uttar Pradesh, India.

- Divya PV and Nandakumar K (2006). Local drug delivery-Periocol in periodontics. Trends Biomater. Artif. Organs. 19: 74-80.

- Dubay DA, Wang X, Kuhn MA, Robson MC and Franz MG (2004). The prevention of incisional hernia formation using a delayed-release polymer of basic fibroblast growth factor. Ann. Surg. 240: 179-86.

- Dufrane D, Mourad M, Steenberghe M, Goebbels RM and Gianello P (2008). Regeneration of abdominal wall musculofascial defects by a human acellular collagen matrix. Biomaterials. 29:  2237-40.

- Eberli D, Atala A and Yoo JJ (2011). One and four layer acellular bladder matrix for fascial tissue reconstruction. J. Mater. Sci. Mater. Med. 22(3):741-51.

- Erkin UR, Kerem M, Tug M, Orbay H and Sensöz O (2007). Prefabrication of a conjoint flap containing xenogenic tissues: a preliminary report on an experimental model. J. Craniofac. Surg. 18: 1451-56.

- Falanga V, Iwamoto S, Chartier M, Yufit T, Butmarc J, Kouttab N, Shrayer D and Carson P (2007). Autologous bone marrow-derived cultured mesenchymal stem cells delivered in a fibrin spray accelerate healing in murine and human cutaneous wounds. Tissue Eng. 13: 1299-1312.

- Freytas DO, Badylak SF, Webster TJ, Geddes LA and Rundell AE (2004). Biaxial strength of multilaminated extracellular matrix scaffolds. Biomaterials. 25: 2353-61.

- Gangwar AK (2002). Biomaterials in repair of abdominal wall defects in rabbits and their clinical application. M.V.Sc. thesis submitted to Indian Veterinary Research Institute, Deemed University, Izatnagar, Bareilly, Uttar Pradesh, India.

- Garfield AS (2010). Derivation of Primary Mouse Embryonic Fibroblast PMEF Cultures, A. Ward and D. Tosh eds., Mouse Cell Culture, Meth. Mol. Biol. 633: 19-27.

- George RS and Mohammad MSD (1993). Studies on diaphragmatic herniorrhaphy with different prosthetic materials. Indian Vet. J. 70: 255-57.

- Germain  L, Auger FA, Grandbois E, Guignard R, Giasson M, Boisjoly H and  Guerin SL (1999). Reconstructed human cornea produced in-vitro by tissue engineering. Pathobiol. 67: 140–47.

- Gianlupi A. and Trindade MRM (2004). Comparison between fixation of polypropylene mesh with polypropylene suture and polyglactin910 suture for treatment of muscle-aponeurotic defects of abdominal wall: experimental study in rats. Acta. Cir. Bras. 19: 94-104.

- Gillion JF, Begin GF, Marecos C and Fourtainiar G (1999). Expanded poly tetra fluoro ethylene patches used in the intraperitoneal or extraperitoneal position for repair of incisional hernias of the anterolateral wall. Am. J. Surg. 174: 16-19.

- Gulati AK and Cole GP (1994). Immunogenicity and regenerative potential of acellular nerve allograft to repair peripheral nerve in rats and rabbits. Acta .Neurochir. Wien. 126: 158-64.

- Hadlock T, Singh S, Vacanti JP and McLaughlin BJ (1999). Ocular cell monolayers cultured on biodegradable substrates. Tissue Engi. 5: 187–96.

- Haichao Yuan,Yue Zhuang, Ju Xiong, Wei Zhi, Liangren Liu, Qiang Wei and Ping Han (2013). Human umbilical mesenchymal stem cells-seeded bladder acellular matrix grafts for reconstruction of bladder defects in a canine model. PLoS ONE 20: 8(12)

- Handley WS (1963). En: Behandlung der Bauchnarbenbrüche. Reitter, H. Langenbecks Arch. Klin. Chir. 304: 296-97.

- Harukazu Tohyama, Toshikazu Yoshikawa, Young-Jin Ju and Kazunori Yasuda (2009). Revascularization in the tendon graft following anterior cruciate ligament reconstruction of the knee: its mechanisms and regulation. Chang Gung. Med. J. 32(2): 133-139

- Hashimoto Y, Funamoto S, Sasaki S, Honda T, Hattori S, Nam K, et al. (2010). Preparation and characterization of decellularized cornea using high-hydrostatic pressurization for corneal tissue engineering. Biomaterials, 31:3941-8.

- Hirotsugu Kurobe, Mark W Maxfield, Christopher K Breuer and Toshiharu Shinoka (2012).  Concise Review: Tissue-Engineered Vascular Grafts for Cardiac Surgery: Past, Present, and Future. Stem Cells Trans. Med. 1(7):566-571.

- Hodde JP and Hiles MC (2002). Virus safety of a porcine-derived medical device: evaluation of a viral inactivation method. Biotechnol. Bioeng. 79: 211–16.

- Huang JH, Cullen DK, Browne KD, Groff R, Zhang J, Pfister BJ, Zager EL, Smith DH (2009). Long-term survival and integration of transplanted engineered nervous tissue constructs promotes peripheral nerve regeneration. Tissue Eng. (Part A) 15(7): 1677-85.

- Indran Balasundaram, Ihsaan Al-Hadad and Sat Parmar (2012). Recent advances in reconstructive oral and maxillofacial surgery. Brit. J. Oral Max. Surg. 50 (8):695-705.

- Ingle-Fehr JE, Baxter GM, Howard RD, Trotter GW and Stashak TS (1997). Bacterial culturing of ventral median celiotomies for prediction of postoperative incisional complications in horses. Vet. Surg. 26: 7–13.

- Ishikawa O, Kondo A, Okada K, Miyachi Y and Furumura M (1997). Morphological and biochemical analyses on fibroblasts and self-produced collagens in a novel three-dimensional culture. Br. J. Dermatol. 1361: 6-11.

- Ivkovic A, Marijanovic I, Hudetz D, Porter RM, Pecina M and  Evans CH (2011). Regenerative medicine and tissue engineering in orthopaedic surgery. Front Biosci. (Elite Ed).  1(3): 923-44.

- Johnson JH (1969).  An evaluation of polypropylene implants in ponies. J. Am. Vet. Med. Assoc. 154: 779–85.

- Joshua P. Aronson, Alim P.Mitha, Brian, L, Hoh, Pavan .K, Auluck, Irina Pomerantseva Joseph P. Vacanti and Christopher S. Ogilvy (2012). A novel tissue engineering approach using an endothelial progenitor cell–seeded biopolymer to treat intracranial saccular aneurysms,Laboratory investigation.  J. Neurosurg. 117(3): 546-554.

- Kaarthick DT (2011). Repair of cutaneous wounds using acellular diaphragm and pericardium of buffalo origin seeded with in-vitro cultured mouse embryonic fibroblast cells in rat model. M. V. Sc. thesis submitted to Indian Veterinary Research Institute, Deemed University, Izatnagar, Bareilly, Uttar Pradesh, India.

- Kanade MG and Kumar A (1990). Mechanical evaluation of Healing of abdominal defects repaired by stainless steel, nylon and cotton mesh in bovine. Indian Vet. J. 67: 47-50.

- Kanade MG, Kumar A and Sharma SN (1988). Repair of abdominal defects by stainless steel and nylon mesh implants in buffaloes: histological and histochemical evaluation. Indian J. Anim. Sci. 58: 415-19.

- Karl FB Payne, Indran Balasundaram, Sanjukta Deb, Lucy Di Silvio, Kathleen FM Fan (2014).  Tissue engineering technology and its possible applications in oral and maxillofacial surgery. Brit. J. Oral Max. Surg. 25(1):7-15.

- Kennedy GM and Matyas JA (1999). Use of expanded polytetrafluroethylene in the repair of the difficult hernia. Am. J. Surg. 168: 304-06.

- Khan WS, Longo UG, Adesida A and Denaro V (2012). Stem cell and tissue engineering applications in orthopaedics and musculoskeletal medicine. Stem Cells Int. 2012: 403170.

- Kneise G (1953). Erfahrungen und neue Erkenntnisebei der Perlonnetz implantation. Central blatt fur. Chir. 12: 506-11.

- Korenkov M, Sauerland S, Arndt M, Bograd L, Neugebauer EA and Troidl H (2002). Randomized clinical trial of suture repair, polypropylene mesh or auto dermal hernioplasty for\ incisional hernia. Br. J. Surg.  89: 50-56.

- Kumar V (2010). Acellular buffalo small intestinal submucosa and fish swim bladder for the repair of full thickness skin wounds in rabbits. M. V. Sc. thesis submitted to Indian Veterinary Research Institute, Deemed University, Izatnagar, Bareilly, Uttar Pradesh, India.

- Kumar V, Gangwar AK, Mathew  DD, Ahamad RA,  Saxena A C, Kumar N (2012). Acellular dermal matrix for surgical repair of ventral hernia. J. Equine Vet. Sci.  334: 238–243.

- Lam MT and Wu JC (2012). Biomaterial applications in cardiovascular tissue repair and regeneration. Expert Rev Cardiovasc. Ther. 10(8):1039-49.

- Lamme, Leeuwen V, Brandsma, Marle V and Middlekoop (2000). Higher numbers of autologous fibroblasts in anartificial dermal substitute improve tissue regeneration and modulate scar tissue formation. J. Path. 1905: 595-603.

- Langer R, Vacanti JP (1993). Tissue engineering. Science. 260 5110: 920–6.

- Lee CH, Singla A and Lee Y (2001). Biomedical application of collagen. Int. J. Pharma. 221: 21-22.

- Lichtenstein IL, Shulman AG and Amid PK (1989). The tension-free hernioplasty. Am. J. Surg. 157:188-193.

- Liu VA and Bhatia SN (2002). Three dimensional photopatterning of hydrogels containing living cells. Biomed. Microdevices.  4:257–266.

- Losanoff JE, Richman BW and Jones JW (2002). Enterocolocutaneous fistula: a late consequence of polypropylene mesh abdominal wall repair: case report and review of the literature. Hernia. 6:144-7.

- Lotze MT (2007).Damage-associated molecular pattern molecules. Clin.Immunol. 124:1–4.

- Lutolf MP and Hubbell JA (2005). Synthetic biomaterials as instructive extracellular microenvironments for morphogenesis in tissue engineering. Nat. Biotechnol. 23: 47-55.

- MacArthur BD and Oreffo RO 2005. Bridging the gap. Nature. 433 7021: 19.

- Maelene L Wong and Leigh G Griffiths  (2014). Immunogenicity in xenogeneic scaffold generation: Antigen removal vs. decellularization. Acta Biomater. 10(5): 1806–1816

- Malangoni MA and Rosen MJ (2007). Hernias. : In Townsend: Sabiston Textbook of Surgery, 18th ed. Chapter 44.

- Malone JM, Brendel K, Duhamil RC and Reinert RL (1984). Detergent- extracted small diameter vascular prostheses. J.  Vasc.  Surg. 1: 181-91.

- Matthew Trese, Caio V Regatieri and Michael J Young (2012). Advances in Retinal Tissue Engineering. Materials 5:108-120.

- Moroni F and Mirabella T (2014). Decellularized matrices for cardiovascular tissue engineering. Am J Stem Cells. 3(1):1-20.

- Mostafa M Kassam, Mahmoud H Elkammer, Ahmed S Korittum and Ali A Abdel-Wahed (2014). Using of Polypropylene Mesh for Hernioplasty in Calves. AJVS.  40(1): 112-117.

- Nagao RJ, Lundy S, Khaing ZZ, and Schmidt CE (2011). Functional characterization of optimized acellular peripheral nerve graft in a rat sciatic nerve injury model. Neurol Res. 33(6):600-8.

- Negro P, Basile F, Brescia A, Buonanno GM, Campanelli G, Canonico S, Cavalli M, Corrado G, Coscarella G and DiLorenzo N (2011). Open tension-free Lichtenstein repair of inguinal hernia: use of fibrin glue versus sutures for mesh fixation. Hernia. 15:  7-14.

- Nelson CM and Bissell M (2006).  Of extracellular matrix, scaffolds and signaling:tissue architecture regulates development, homeostasis and cancer. Annu. Rev. Cell. Dev. Biol. 22: 287-309.

- Onkar Singh, Shilpi Singh Gupta, Mohan Soni, Sonia Moses, Sumit Shukla, and Raj Kumar Mathur (2011). Collagen dressing versus conventional dressings in burn and chronic wounds: A retrospective study. J. Cutan. Aesthet. Surg.  4(1): 12–16.

- Pang K, Du L, Wu X (2010). A rabbit anterior cornea replacement derived from acellular porcine cornea matrix, epithelial cells and keratocytes. Biomaterials. 31:7257-65.

- Penttinen R and Grönroos JM (2008). Mesh repair of common abdominal hernias: a review on experimental and clinical studies. Hernia. 12: 337–344.

- Perme H (2007). In-vitro and in-vivo biocompatibility of cross-linked bovine pericardium and diaphragm. M. V. Sc. thesis submitted to Indian Veterinary Research Institute, Deemed University, Izatnagar, Bareilly, Uttar Pradesh, India.

- Pu F, Rhodes NP, Bayon Y, Chen R, Brans G, Benne R and Hunt JA (2010). The use of flow perfusion culture and subcutaneous implantation with fibroblast-seeded PLLA-collagen 3-D scaffolds for abdominal wall repair. Biomaterials. 31: 4330-40.

- Purohit S (2008). Biocompatibility testing of acellular dermal grafts in a rabbit model: An in-vitro and in-vivo study. Ph. D. thesis submitted to Indian Veterinary Research Institute, Deemed University, Izatnagar, Bareilly, Uttar Pradesh, India.

- Read RC (2011). Crucial steps in the evolution of the preperitoneal approaches to the groin: a historical review. Hernia. 15: 1-5.

- Reginald C W Bell, Jacqueline Fearon, and Katherine D Freeman (2013). Allograft dermal matrix hiatoplasty during laparoscopic primary fundoplication, paraesophagal hernia repair, and reoperation for failed hiatal hernia repair. Surg. Endosc. 27(6): 1997-2004.

- Remya V (2012).Tissue engineered fish swim bladder scaffold seeded with bone marrow derived mesenchymal stem cells of rat and goat for dermal tissue reconstruction. M. V. Sc. thesis submitted to Indian Veterinary Research Institute, Deemed University, Izatnagar, Bareilly, Uttar Pradesh, India.

- Rennekampff HO, Kiessig V, Griffey S, Greenleaf G and Hansbrough JF (1997). Acellular human dermis promotes cultured keratinocyte engraftment. J.  Burn Care Rehabil. 18: 535-38.

- Ripley WA and McCarnan (1974). Umbilical hernia repair with mersilenemesh. Canadian Vet. J. 15: 357-61.

- Rosenberg AS, Mizuochi T, Sharrow SO and Singer A (1987). Phenotype, specificity and function of T cell subsets and T cell interactions involved in skin allograft rejection. J. Exptl. Med. 165: 1296-99.

- Rousch JK (2003). Biomaterials and surgical implants. In Textbook of small animal surgery. Edited by Slatter, D. H., 3rdedn. Saunders, Philadelphia, USA. Pp141-48.

- S J Kew, JH Gwynne, D Enea, M Abu-Rub, A Pandit, D Zeugolis, RA Brooks, N Rushton, SM Best and RE Cameron (2011). Regeneration and repair of tendon and ligament tissue using collagen fibre biomaterials. Acta Biomater. 7(9): 3237-3247.

- Schmidt CE and Baier JM (2000). Acellular vascular tissue: natural biomaterials for tissue repair and tissue engineering. Biomaterials. 21: 2215-31.

- Schoen FJ (2011). Heart valve tissue engineering: quo vadis? Current Opinion in Biotechnology. 22:698-705.

- Seddon AM, Curnow P and Booth PJ (2004). Membrane proteins, lipids and detergents: not just a soap opera. Biochem. Biophys. Acta. 166: 105–17.

- Sheridan WS, Duffy GP, and Murphy BP (2013). Optimum parameters for freeze-drying decellularized arterial scaffolds. Tissue Eng. Part C Methods. 19(12):981-90.

- Shi C, Chen W, Zhao Y, Chen B, Xiao Z, Wei Z, Hou X, Tang J, Wang Z and Dai J (2011). Regeneration of full-thickness abdominal wall defects in rats using collagen scaffolds loaded with collagen-binding basic fibroblast growth factor. Biomaterials. 32: 753-59.

- Shoukry M, El-Keiey M, Hamouda M and Gadallah S (1997). Commercial polyester fabric repair of abdominal hernias and defects. Vet. Rec. 140: 606-07.

- Silva HC, Silva AL and Oliveira CM (2004). Peritoneum autogenous graft fibroblast: an experimental study. Rev. Col. Bras. Cir. 31: 83-89.

- Stock FE (1954). Repair of large hernia with nylon mesh. Lancet. 10: 395.

- Stoppa RG and Rives J (1984). The use of dacron in the repair of hernias of the groin. Surg. Clin. North América. 64: 269-85.

- Takahashi M, Ono K, Wakakuwa R, Sato O, Tsuchiya T, Kamya G, Nitta K, Tajima K and Wada K (1994). Use of human dura matter allograft for the repair of a contaminated abdominal wall defect. Surg. Today.  24: 468- 72.

- Turner NJ, Valentin JE, Sicari BM and Badylak SF (2011). Biologic Scaffolds for Skeletal Muscle Reconstruction.  Department of Surgery, University of Pittsburgh, USA
 Poster Session II.

- Umile Giuseppe Longo, Alfredo Lamberti, Nicola Maffulli and Vincenzo Denaro (2010).  Tendon augmentation grafts: a systematic review. Br. Med. Bull. 94 (1): 165-188.

- Usher FC, Ochsner J and Tuttle LL (1958).  Use of Marlex mesh in the repair of incisional hernias. J. Am. Surg. 24: 969–74.

- Van der Veen V, Van der Wal MB, Van Leeuwen MC, Ulrich MM and Midelkoop E (2010). Biological backgroud of dermal substitutes. Burns. 36: 305-21.

- Vilar JM, Doreste F, Spinella G and Valentin S (2009). Double layer mesh hernioplasty for repair of incisional hernias in 15 horses. J. Equine Vet. Sci.  29: 172–76.

- Wang S, Goecke T, Meixner C, Haverich A, Hilfiker A, and Wolkers WF (2012). Freeze-dried heart valve scaffolds. Tissue Eng. Part C Methods. 18(7):517-25.

- Witzel O (1900) Uber den verschluss van bauchwunden und bruchp fortendurch versenktesilberdrahtnetze. Zetralbl. Chir. 27: 3.

- Yannas IV (1996).  Natural materials. In: Ratner BD, Hoffman AS, Schoen FJ, Lemon J E, editor. Biomaterial Science, Academic Press, San Diego. pp 84-94.

- Yoo JJ, Meng J, Oberpenning F and Atala A (1998).  Bladder augmentation using allogenic bladder submucosa seeded with cells. Urology. 51: 221–25.

- Youssef Aachoui and Swapan K Ghosh (2011). Extracellular matrix from porcine small intestinal submucosa (sis) as immune adjuvants. PLoS ONE, 8(12) DOI: 10.1371/journal.pone.0027083

- Yusuke Sakai, Makiko Koike, Hideko Hasegawa, Kosho Yamanouchi, Akihiko Soyama, Mitsuhisa Takatsuki, Tamotsu Kuroki, Kazuo Ohashi, Teruo Okano, Susumu Eguchi (2013). Rapid Fabricating Technique for Multi-Layered Human Hepatic Cell Sheets by Forceful Contraction of the Fibroblast Monolayer.  PLoS ONE 8(12).

- Zang M, Zhang Q, Chang EI, Mathur AB and Yu P (2012). Decellularized tracheal matrix scaffold for tissue engineering. Plast. Reconstr. Surg. 130(3):532-40.

- Zhang F,  Zhang J, Lin S, Oswald T, Sones W, Cai Z, Dorsett-Martin W and Lineaweaver WC (2003). Small intestinal submucosa in abdominal wall repair after TRAM flaps harvesting in a rat model. Plast. Reconstr. Surg. 112: 565-70.

- Zhang M, Wang Y, Wang D, Pan Y and Chen J (2002). Studies on xenogenic acellular dermal matrix as filling material. Zhonghua Zheng  Xing Wai Ke Za Zhi. 18: 263-65.

- Zhao YY, Zhang ZZ, Wang JJ, Yin PP, Zhou JJ, Zhen MM, Cui WW, Xu GG, Yang DD and Liu ZZ (2012). Abdominal hernia repair with a decellularized dermal scaffold seeded with autologous bone marrow-derived mesenchymal stem cells. Artif. Organs. 36: 247-55.

- Zhu WD, Xu YM, Feng C, Fu Q, Song LJ and Cui, L (2010). Bladder reconstruction with adipose-derived stem cell-seeded bladder acellular matrix grafts improve morphology composition. World J. Urol. 28: 493–498.